## Slide 1: Background analysis techniques in the cuore experiment
Barbara S. Wang, on behalf of the CUORE Collaboration
Low Radioactivity Techniques 2015 Workshop
Seattle, WA
March 18 – 20, 2015

## Slide 2: Cuore detector
Cryogenic Underground Observatory for Rare Events (CUORE)
  Will search for 0νββ decay of 130Te (Q-value = 2528 keV)
  Detector is an array of 988 natural TeO2 bolometers:
    19 towers; 13 floors/tower; 4 bolometers/floor
    741 kg total; 206 kg 130Te
    Isotopic abundance of 130Te is 34%
    Array will be held in a cryostat and cooled to ~10 mK
  Data taking to start in late 2015.

## Slide 3: Bolometric technique
Typical CUORE pulse
TeO2 bolometers:
  Particle interaction deposits energy in crystal.
  Resulting temperature rise (∆T) measured.
  Energy deposition determined from E = C ∆T (C is heat capacity).
0νββ decay signature: peak at Q-value
  Energy resolution at 2528 keV: FWHM ~ 5-7 keV
ΔE/Q
Counts
0νββ
2νββ
Not to scale

## Slide 4: Half-life sensitivity

## Slide 5: Half-life sensitivity
CUORE
Background Goal
y
Corresponds to mββ = 51-133 meV (90% C.L.)

## Slide 6: Background analysis techniques
Gamma spectroscopy w/ HPGe detectors
Neutron activation analysis
Alpha spectroscopy w/ Si surface barrier detectors
ICP-MS
Bolometry w/ TeO2
Cross-section measurements for cosmogenic-isotope production in detector materials (e.g., Te)
Data-analysis cuts
Monte Carlo simulations
Notes:   Bolometry w/ TeO2 (able to reach sensitivities of a few nBq/cm3)

## Slide 7: Background spectra
2003-2008
March 2013-Spring 2015
0νββ region
Gammas, betas
alphas
M1 spectra
M1 spectra
Only events that occur in a single crystal are plotted. These are known as multiplicity 1 (M1) events.

## Slide 8: Neutrinoless double-beta decay region
0νββ-decay region:
Excellent energy resolution (~5 keV) at 2528-keV Q value allows the 0νββ-decay peak to be unambiguously distinguished from the 60Co sum peak.
M1 spectrum

## Slide 9: Alpha background
Alpha decay: Qα = Eα + ER
Alpha background comes from
  Bulk contamination of TeO2 crystals
    Deposits Qα in crystal
  Surface contamination of TeO2 crystals
    Fully contained event: deposits Qα in crystal.
    Partially contained event: alpha (or recoil) loses energy in crystal before escaping completely or depositing remaining energy in an adjacent crystal
  Surface contamination of the copper frames
    Alpha loses energy in copper before depositing remaining energy in TeO2 crystal
“Degraded” alphas:
  Alphas that deposit partial energy in the crystals
  Background extends from Qα or Eα down to zero

## Slide 10: Alpha background
Crystal bulk and surface events can be disentangled by comparing spectra for single-crystal events (M1) with those for two-crystal events (M2)
Energy deposited in individual crystals during each event is plotted
Energy deposited in entire detector array during each event is plotted

## Slide 11: Alpha background
Degraded-alpha signature from Po-210 surface contamination on copper
Simulation results for different contamination thicknesses shown
Energy deposited in individual crystals during each event plotted
M1
M2

## Slide 12: Gamma/beta region
Dominated by Th-232 and U-238 contaminations in the cryostat and/or its shields.
e+e- annihilation
214Bi
40K
208Tl
60Co
228Ac
CUORE-0
M1 spectrum
0νββ

## Slide 13: Background model and monte carlo simulations
Three major contributors to 0νββ-decay region:
  10 ± 5%: U-238 and Th-232 surface contaminations of crystals
  50 ± 20%: Th-232 surface contaminations of copper (or any other component facing crystals)
  30 ± 10%: multi-Compton events from Tl-208 2614 keV line (due to Th-232 contamination in cryostat)
M1 spectra

## Slide 14: Improving the alpha background
CUORE-0 has achieved an overall background 2 times lower than Cuoricino and an alpha background 6 times lower.
Due largely to more rigorous copper cleaning methods and more consistent cleaning protocol for crystals.
M1 spectra
First results from CUORE-0 published in The European Physical Journal C 74, 2956 (2014)

## Slide 15: Cosmogenic background
Background from 110mAg and 60Co present due to cosmogenic activation of TeO2 crystals.
Background estimated using radioisotope-production cross sections measured at the Los Alamos Neutron Science Center (LANSCE).
  TeO2 powder irradiated w/ a neutron spectrum similar in shape to the cosmic-ray neutron spectrum at sea-level.
  Cross sections obtained1: 110mAg: 0.28 ± 0.04 mb, 60Co: < 0.0016 mb
1 Paper on the cross-section measurement submitted to Physical Review C. Preprint may be found here: http://arxiv.org/abs/1503.02095

## Slide 16: Background budget

## Slide 17: Thank you for listening. Questions?