## Slide 1: The Ultratrace Determination of Th and U in a Variety of Detector Materials and Components for Use in Ultralow Background Applications
Isaac Arnquist, Brian LaFerriere, tapas maiti, eric hoppe
Pacific Northwest National Labs
LRT Conference

## Slide 2: The Setup
ICP-MS analysis for the radionuclide determination in detector components
Isotope dilution analysis using radioactive tracers for U and Th
  Gold standard for quantitation
  229Th, 233U
Utilize Class 10,000 Cleanroom and Class 10 laminar flowhoods

## Slide 3: A Smörgåsbord of Samples
Structural and Shielding Components
  Cu, Pb, Ti, and Stainless Steel is becoming more routine at lower and lower levels
Specialty Components
  Fused Silica
  Electronic Components
  Linear Alkyl Benzene
  Particulates from filters
  Polymers

## Slide 4: Fused Silica
Absolute Detection Limits (pg) | 
Th-232 | U-238
0.250 | 0.308
 |  | Th-232 |  | U-238 | 
Sample Name | Rep# | pg/g fused silica | mBq/kg | pg/g fused silica | mBq/kg
Lot_A | Rep1 | <2.26 | <9.25 | 40.4 | 501
Lot_A | Rep2 | 2.82 | 11.6 | 41.6 | 516
Lot_A | Rep3 | 4.13 | 16.9 | 42.0 | 521
Lot_B | - | <2.26 | <9.25 | 37.3 | 463
Lot_C | - | <2.26 | <9.25 | 5.76 | 71.4
Lot_D | - | 2.86 | 11.7 | 6.83 | 84.7
Lot_E | - | 6.12 | 25.1 | 68.4 | 849
Lot_F | Rep1 | 11.9 | 48.7 | 123 | 1527
Lot_F | Rep2 | 12.5 | 51.2 | 101 | 1250
Lot_F | Rep3 | 10.8 | 44.3 | 133 | 1645
Sample Size: 70-150 mg
Dissolution in concentrated HF and HNO3
  SiO2 + 4 HF  SiF4(g) + 2H2O

## Slide 5: Electronic Components
 | Th-232 |  | U-238 | 
Sample | pg/piece | mBq/kg | pg/piece | mBq/kg
Millmax Small Socket1 | 248 | 51.6 | 1083 | 682
Millmax Small Socket2 | 263 | 52.1 | 1139 | 682
Millmax Large Socket1 | 310 | 35.1 | 1390 | 477
Millmax Large Socket2 | 300 | 33.5 | 1421 | 480
Millmax Pin1 | 1.80 | 0.220 | 0.704 | 0.260
Millmax Pin2 | 1.70 | 0.203 | 1.06 | 0.384
SQUID1 | 1.40 | 0.342 | 0.20 | 0.147
SQUID2 | 0.326 | 0.0793 | 0.177 | 0.130
SQUID3 | 0.189 | 0.0459 | 0.0569 | 0.0418
5k W Resistor | 0.0352 | - | 0.0160 | -
80 MW Resistor | 0.237 | - | 0.111 | -
10 nF Capacitor | 0.0861 | - | 0.0274 | -
HEMT | 0.0670 | - | 0.0557 | -
0 W Resistor | 236 | - | 104 | -
RuOx Thermometer | 817 | - | 407 | -
5 mW Resistor | 17.0 | - | 109 | -
3.75 pF Capacitor | 2.12 | - | 0.492 | -
Absolute Detection Limits (pg) | 
Th-232 | U-238
0.1-0.6 | 0.1-0.4
Sample Size: 0*-35 mg
Dissolution in concentrated HNO3, HF, and/or HCl
RuOx Thermometer
10 nF Capacitor, 5 mOhm Resistor, & 3.75 pF Capacitor components
L-R: Millmax large and small sockets and pin

## Slide 6: Linear Alkyl Benzene (LAB)
Absolute Detection Limits (fg) | 
Th-232 | U-238
54.8 | 33.7
 |  | Th-232 |  | U-238 | 
Sample Name | Rep# | fg/g LAB | mBq/kg | fg/g LAB | mBq/kg
LAB_A | 1 | <6.61 | <0.0271 | 13.0 | 0.161
LAB_A | 2 | <6.39 | <0.0262 | 14.6 | 0.181
LAB_A | 3 | <6.43 | <0.0264 | 11.8 | 0.147
LAB_B | 1 | <6.55 | <0.0269 | <4.03 | <0.0499
LAB_B | 2 | <6.43 | <0.0263 | <3.95 | <0.0490
LAB_B | 3 | <6.35 | <0.0260 | <3.90 | <0.0484
LAB_C | 1 | 52.1 | 0.214 | 19.6 | 0.243
¥ Image from: http://commons.wikimedia.org/wiki/File:Linear_alkylbenzene.png#/media/File:Linear_alkylbenzene.png
¥
LAB_A
LAB_B
LAB_C
Liquid scintillator with high optical transparency
Very low vapor pressure
  b.p. ~300oC
Sample Size: ~8.5 grams

## Slide 7: Filter Particulates
Absolute Detection Limits (pg) | 
Th-232 | U-238
0.607 | 0.497
 | Th-232 | U-238
Sample | pg/filter | pg/filter
Filter_A | <0.607 | <0.497
Filter_B | 7.30 | 0.584
Filter_C | 234 | 10.8
PTFE filters with captured particulates were analyzed for U, Th
Sample and blank filters were subjected to particulate dissolution using a mixture of HNO3 and HF

## Slide 8: Polymethyl Methacrylate (PMMA)
Absolute Detection Limits (fg) | 
Th-232 | U-238
27.5 | 21.0
 | Th-232 |  | U-238 | 
Sample | fg/g PMMA | mBq/kg | fg/g PMMA | mBq/kg
PMMA1 | <183 | <0.750 | 154 | 1.91
PMMA2 | 269 | 1.10 | 202 | 2.51
PMMA3 | <182 | <0.746 | 162 | 2.01
Dry-ash PMMA in ultralow background electroformed copper crucibles using a tube furnace under air flow (2L/min)
Dissolve crucible/residue and isolate U, Th using anion exchange separation¥
¥ B.D. LaFerriere et al. / Nuclear Instruments and Methods in Physics Research A 775 (2015) 93-98.
Method will be presented at the MARC X conference in April 2015

## Slide 9: Conclusions
ICP-MS and well-crafted sample preparation methodology allows for the analysis of specialty components important in ultralow background physics experiments
  Microgram-samples
  Nonpolar compounds
  Polymers

## Slide 10: Acknowledgments
Eric Hoppe
Brian LaFerriere
Tapas Maiti
May-Lin Thomas
Jay Grate
Mary Bliss
Jeter Hall
John Orrell

## Slide 11
Questions?